## Slide 1: PPG POWERCRON® 6th-generation family of cationic epoxy electrocoats

## Slide 2: Electrocoat organization
Thor Lingenfelter
Substrate Protection Technical Manager
Springdale, PA / Euclid, OH
25 years in Electrocoat
Andrea Gray
Substrate Protection Industrial Coatings Team Leader
Springdale, PA / Euclid, OH
14 years in Electrocoat

## Slide 3
Electrocoat basics

## Slide 4: Where is electrocoat used?
Military
Compressors
Marine engines
Agriculture and Construction
Automotive parts
Trucks and buses
Suspension components
Castings and pipes
Transformers
Switchgear
Fasteners
HVAC

## Slide 5: Why use electrocoat?
Economical and Efficient
High transfer efficiency
Precise film build control
100% coverage of complex parts
Coats recessed areas
Automated system: low maintenance and minimal labor
Dense racking of parts
Non-uniform line loading
Environmentally Conscientious
Low VOC options available
Specifically formulated without HAPs
Minimal waste discharge
Water-based formulations
Workers have minimal contact with materials
Excellent Performance
Controlled uniform film thickness
Improved aesthetics
No runs, drips or sags
100% coverage
One- or two-coat applications for optimal performance
Epoxy-based for corrosion, acrylic-based for durability
Some Disadvantages
Capital expenditure
Color flexibility (multiple colors)
Substrate must be conductive
Bake required (thermoset)

## Slide 6: Electrocoat technologies
Acrylic
Color and gloss control for interior products
Metal office furniture, air diffusers, range hoods, toolboxes
Epoxy
Low-bake applications
Heavy-duty castings, compressors
Acrylic
High performance, one-coat applications
UV durability and detergent resistance
Color control
Epoxy
Benchmark for corrosion and chemical resistance
Automotive parts, car bodies, heavy duty trucks, fasteners
Electrocoat Product Choice – PPG 6th Generation
Cathodic
Anodic

## Slide 7: Versatile protection and performance options
E-coat primer + liquid or powder
Electrocoat dual-coat
Electrocoat + a liquid or powder topcoat produces exceptional performance properties
Two electrocoat layers for high performance
Electrocoat monocoat
Electrocoat is the final finish – no UV exposure

## Slide 8
Powercron 6th-generation family of electrocoats

## Slide 9: PPG historic cationic e-coat development
1960s
1970s
1990s
2000
2001
2006
2007
2015
First cathodic auto body tank
Improved corrosion and throwpower
POWERx®: Comprehensive system to control bacteria
Powercron 8000: Lower VOCs and lower cure than previous generations
PPG POWERCRON® ADVANTEDGE™: Organic catalyst, reduced cure, one component, high edge product
First automotive body tank (anodic)
Single-Component Powercron 6000CX: Workhorse product now with improved quality, simplicity and reduced material handling
2009
Powercron 6100HE: High edge coverage, cathodic epoxy electrocoat
Powercron XP: Formulated specifically for fastener applications with built-in torque control
Ultrafiltration
Cathodic epoxy: specifically formulated without HAPs and lead
Single component P590-534
Powercron 6000CX: Workhorse cationic epoxy product, noted for robust operation and workability
* Not intentionally added.

## Slide 10: PPG Powercron 6th-generation family of cationic epoxy electrocoats
Single- or two-component feed packages with metal-based catalysts
Range of products offering standard and high-edge protection of complex parts
Multiple throwpower options
VOC options as low as < 0.3 lbs./gal. (36 g/L) as supplied
Low-cure products that may lower energy use
Black, gray and color options available (not controlled)
Major OEM approvals simplify specification process and broaden potential customer base
✔
1K 2K

## Slide 11: Full product family
 | Core Products |  |  | Specialty Products | 
 | FrameCoat II | Powercron 6100HE | Powercron 6000CX | Powercron XP/SL | Powercron CD
Markets | Automotive parts and accessories | Automotive parts and accessories General industrial Heavy duty equipment Transportation | Automotive parts and accessories General industrial Heavy duty equipment Appliance Transportation | General industrial (fasteners) | General industrial (power/electrical)
Special Benefits | Specially formulated for frames High-edge coverage of complex/sharp parts Improved surface profile versus competing electrocoats | High-edge coverage of complex/sharp parts NSF-approved and torque-modified formulations available | Standard coverage of densely racked parts | High-edge coverage of threads and edges Additives for lessening touch marks Torque-modified versions available | Conductive epoxy platform for 2-coat electrocoat Formulated for extreme environments

## Slide 12: Core products
Product Characteristics | FrameCoat II | Powercron 6100HE | Powercron 6000CX
Feed package | 2K | 2K | 1K or 2K
Cure | 350˚ F (177˚ C) for 20 min. | 350˚ F (177˚ C) for 20 min. | 350˚ F (177˚ C) for 20 min.
VOCs as Supplied | VOCs < 0.3 lbs./gal. (36 g/L) | VOCs < 0.3 lbs./gal. (36 g/L) | VOCs < 0.2 lbs./gal. (24 g/L)
Color | Black or gray | Multiple colors (not controlled) | 1K: black 2K: multiple colors (not controlled)
Gloss at 60˚ (ASTM D523) | 50 – 80 | 50 – 80 | 65 – 85
Dry Film Thickness (ASTM D7091) | 0.5 – 1.5 mils | 0.5 – 1.5 mils | 0.4 – 1.5 mils
Performance Properties* |  |  | 
Pencil Hardness (ASTM D3363) | 2H minimum | 2H minimum | 2H minimum
Direct Impact (ASTM D2794) | 100 in.-lbs. minimum | 100 in.-lbs. minimum | 100 in.-lbs. minimum
Reverse Impact (ASTM D2794) | 60 in.-lbs. minimum | 60 in.-lbs. minimum | 60 in.-lbs. minimum
Humidity Resistance (ASTM D1735) | 1,000 hours minimum | 1,000 hours minimum | 1,000 hours minimum
Gravelometer (OEM performance standard) | 6 minimum | 6 minimum | 6 minimum
Rust Spot (OEM performance standard) | <5 average | <5 average | 40 – 60
Crosshatch Adhesion (ASTM D3359) | 4B – 5B | 4B – 5B | 4B – 5B
Water Immersion (ASTM D870) | 250 hours minimum | 250 hours minimum | 250 hours minimum
Throwpower (OEM performance standard) | 12 – 15 inches | 12 – 15 inches | 12 – 15 inches
Corrosion Performance (1,000 Hrs. ASTM B117) | 1 – 2 mm | 1 – 2 mm | 1 – 2 mm
* Testing performed on cold-rolled steel lab panels with zinc-phosphate pretreatment, 0.8 mils average film thickness, 20-minute cure at 320˚ F (160˚ C).

## Slide 13
Corrosion performance

## Slide 14: Corrosion performance*
 | Salt Spray (1,000 hours) | OEM Scab Testing (28 cycles) | SAE J2334 (40 cycles)
Powercron 6100HE | 1.2 mm | 4.3 mm | 3.4 mm
Competitor A | 1.2 mm | 5.1 mm | 4.2 mm
* Tests performed on cold-rolled steel lab panels with zinc phosphate pretreatment, 0.9 mils average film thickness, unless otherwise noted.
** Test performed on galvanized steel lab panels with zinc phosphate pretreatment, 1.3 mils average film thickness.
 | Salt Spray (500 hours) | OEM CCT Testing (30 cycles)** ► | SAE J2334 (30 cycles)
FrameCoat II | 0.52 mm | 0.87 mm | 2.90 mm
Competitor B | 0.70 mm | 1.31 mm | 3.34 mm
FrameCoat II
Competitor B
OEM CCT Testing (30 cycles)**

## Slide 15
Throwpower

## Slide 16: Throwpower performance
Shim Test Method
 | Throw
FrameCoat II | 65%
Competitor B | 57%
Through bolt for panel connection
¼” spacer
Outer panel
Inner panel

## Slide 17: Throwpower performance
25
20
15
10
5
0
A
B
C
D
E
F
G
Box Throwpower Method
Faces A-G DFT • Comparison at A=20µ
Competitor N
Competitor K
Powercron 6100HE

## Slide 18
Edge protection

## Slide 19: Edge corrosion performance
Punched Hole: 1,000 Hours in Salt Spray
Powercron 6000CX
Standard-edge electrocoat
Powercron 6100HE / FrameCoat II
High-edge electrocoat

## Slide 20: Edge corrosion performance
20 mm
3 mm
Powercron 6000CX
Standard-edge electrocoat
Powercron 6100HE / FrameCoat II
High-edge electrocoat
Cross-Section of Coated Edges

## Slide 21: Edge corrosion performance
20 μm DFT
Cast-Iron Options / Success in Corrosion
Powercron 6000CX
Standard-edge electrocoat
Powercron 6100HE / FrameCoat II
High-edge electrocoat
40 μm DFT
20 μm DFT

## Slide 22: Edge corrosion performance
 | Knife Blade Edge Corrosion | Laser Cut Edge Panels
Powercron 6100HE | 6-10 rust spots | < 0.5% edge corrosion
Competitor A | 50-60 rust spots | > 50.0% edge corrosion
Salt Spray Testing (720 hours, cold-rolled steel)
Powercron 6100HE vs. Competitor A

## Slide 23: Edge corrosion performance
FrameCoat II
Competitor A
Salt Spray Testing (1 week, 1.0 mil dry film thickness)
 | Knife Blade Edge Corrosion
FrameCoat II | 5-7 rust spots
Competitor A | 55-75 rust spots

## Slide 24
Other considerations

## Slide 25: Powercron 6th-generation family operating versatility*
Wide solids range; can adjust outside typical range based on specific customer needs
Minimal over-the-side additions needed (solvents, etc.)
Historically lower prevalence of bio-activity and appearance issues with preventative maintenance compared to other electrocoat generations
Two decades of proven excellence
* Normal operating ranges are always recommended for best performance.

## Slide 26: Conversions from competitors to Powercron family products
Successful top feeds completed over:
  Competitor A
  No conversion issues documented
  Competitor B
  May need solvent addition for smooth film during conversion process; some improved filterability as conversion continues

## Slide 27: Electrocoat organization
Derek Kovacs
APA Team Leader
Dave Junker
Analytical / Tank Sampling
Kim Decheck
Performance Testing
Gary Orosz
Engineering / Equipment
Lisa Ventrano
Product Management Americas

## Slide 28: Thank You
Andrea Gray
Substrate Protection Industrial Coatings Team Leader
agray@ppg.com
Thor Lingenfelter
Substrate Protection Technical Manager
lingenfelter@ppg.com